Hydrogen storage materials for energy saving and low CO2 emission: microstructural refinement by HPT for high performance

Zenji Horita1,2

1 Department of Materials Science and Engineering, Faculty of Engineering, Kyushu University, Fukuoka 819-0395, Japan

2 WPI International Institute for Carbon-Neutral Energy Research (WPI-I2CNER), Kyushu University, Fukuoka 819-0395, Japan

High performance of hydrogen storage requires not only fast absorption/desorption kinetics but also lower operating temperature near ambient pressure. A process of severe plastic deformation through high-pressure torsion (HPT) were applied to two major hydrogen storage metallic materials such as Ti-based and Mg-based systems. Microstructures were well refined by the HPT process so that nanograins were formed in the materials. For the Ti-based system, an HPT-processed TiFe intermetallic no longer requires pre-activation that limits practical use as it involves exposure to hydrogen atmosphere under high pressures (>3 MPa) at high temperatures (~450oC). No requirement for the pre-activation is because hydrogen diffusion is enhanced through introduction of high densities of lattice defects such as grain boundaries [1]. Furthermore, the HPT-processed TiFe was not deactivated even after storage in air [2]. Application of the HPT process to Mg2Ni made its hydrogen storage performance improved so that hydrogen absorption is feasible at a reduced temperature as 423 K with faster hydrogen kinetics. This was due to the introduction of high densities of planar lattice defects such as grain boundaries and stacking faults [3].

[1] K. Edalati, J. Matsuda, H. Iwaoka, S. Toh, E. Akiba, Z. Horita, Int. J. Hydrogen Energy 38 (2013) 4622-4627.

[2] K. Edalati, J. Matsuda, M. Arita, T. Daio, E. Akiba, Z.Horita, Appl. Phys. Lett. 103 (2013) 143902.

[3] T. Hongo, K. Edalati, M. Arita, J. Matsuda, E. Akiba, Z. Horita, Acta Mater. 92 (2015) 46-54.